Introduction

Flame Paint Additive is a concentrate used to create a Surface Spread of Flame resistant coating from an ordinary paint.

Flame Paint Additive should be well mixed into any normal water or oil based paint, at the rate of one pot of the relevant size per 2.5 litres or 5 litres of paint.

Special features

- Water based

- No odour

- Clear

- Can be added to any Paint, but NOT Varnishes

- Changes paint into a Class 1 Flame Paint

DESCRIPTION

Flame Paint Additive is a one part concentrate used to convert ordinary paint into a Class 1 Flame Paint. It produces a safe, inert gas in a fire, to extinguish surface spread of flame.

TECHNICAL DATA

Active Substance

Anti Flame Gas Generating Concentrate

Coverage

Use one pot per 2.5/5.0 litres of paint

Pot Size

Gross weights – 45 grams/68 grams

Aggressivity to other materials

None known

Classification

Non toxic – not hazardous

Mixing

Stir thoroughly into your chosen paint.

Fire Testing

Tested to BS476 Part 7; Class 1 Surface Spread of Flame.

Spraying Flame Paints

Airless spray – Graco 1500 or 5000 with 0.015" tip. Pressure pot – Devilbiss J.G.A 502 gun, 402-FF needle, 705 aircap, FF nozzle.

PRS Flame Paint

Additive Concentrate

ADDITIVE CONCENTRATE

MODIFIES ANY PAINT TO CLASS 1

Property Repair Systems

01626 331351

USES

Fire Proofing top coat Additive for Flame Paint Applications, for Class 1 Paint to be applied to plasterboard and timber materials on walls and ceilings, indoors and outdoors.  Also for paints to be applied directly to plywood, chipboard, MDF, fibreboard and other man-made timber based boards.

PREPARATION & METHOD

Stir the standard paint thoroughly first.

Scoop out the Flame Paint Additive concentrate with a spoon or pallet knife.

Stir very thoroughly again, preferably with a mixing paddle in an electric drilling machine.

Apply the paint to a well prepared, flatted, grease free surface or over an Intumescent Paint. Ensure that the Intumescent Paint is completely dry and hard before coating.

Allow to dry hard before applying a second coat.

Property Repair Systems - 01626 331351

Unit 3, Olympus Business Park, TQ12 2SN